## Slide 1: 3D Printed FlexMask V1
The following presentation is a compilation of designs, notes, and instructions for printing and assembling a FlexMask
Andrew Przyjemski
awp5357@psu.edu

## Slide 2: Materials

## Slide 3: Bill of Materials
TPU95 flexible filament
540 mm of 1.5mm aluminum armature wire
Straps (examples listed below)
  4mm ID x 6mm OD Silicone rubber tube
  Non-latex resistance band
  Other strap materials are feasible, but only the two above have been tested

## Slide 4: Cost of Goods Sold (COGS)
Item | Supplier | Category | Price | Link
1.5mm x 550mm Armature wire | Animation Toolkit | Armature | $0.17 | https://tinyurl.com/yx7r4c38
Elastic cord 1/8” x 30” | Amazon | Strap | $0.04 | https://tinyurl.com/tf4ujzb
Polymaker PolyFlex 750 gram roll | Polymaker | Base | $1.80 | https://tinyurl.com/uvtl5es
Filter | ??? | Filter | ??? | ???

## Slide 5: 3D Printing

## Slide 6: Slicing Settings
Material: Polymaker PolyFlex
  Extruder: 250°C
  Bed: 60°C
Layers and perimeters
  Layer height: 0.3mm
  # Perimeters: 2
  Solid layers: 3 top and bottom
Infill
  Density: 25%
  Pattern: Rectilinear
Speed
  20mm/s for all speed settings
Print time: ≈3 hours
Material Used: 34 grams
Print Orientation

## Slide 7: Printed Mask

## Slide 8: Assembly

## Slide 9: Assembly Materials
2 x (1.5mm x 210mm Al wire)
1 x (1.5mm x 120mm Al wire)
1 x 500mm strap (top)
  Length may vary based on head size and strap material
1 x 330mm strap (bottom)
  Length may vary based on head size and strap material
220mm x 180mm filter media
  ≈ 1/8” thick preferable

## Slide 10: Assembly Materials

## Slide 11: Assembly
Fold filter media along long dimension to form two pleats. Total length should be between 100 and 110mm
The filter media used in this presentation is cheesecloth and is used only for demonstration.
Cheesecloth is NOT an acceptable filter media for medical use.

## Slide 12: Assembly
Insert 210mm armature wires through the channel on each side of the mask, leaving 50mm at the bottom
50mm
50mm

## Slide 13: Assembly
Bend wires 90 degrees

## Slide 14: Assembly
Flip over and insert short armature wire through the channel on the nose bridge

## Slide 16: Assembly
Tie straps to each strap hole, with the longer band being tied to the top half of the mask
Top band

## Slide 17: Assembly
Place pleated filter media on the back (flat side) of the mask

## Slide 18: Assembly
Fold down armatures so the filter media is held in place

## Slide 20: Assembly
Place on face and bend nose bridge armature to ensure proper fit