## Slide 1: 3D Printed FlexMask V1
The following presentation is a compilation of designs, notes, and instructions for printing and assembling a FlexMask
Andrew Przyjemski
awp5357@psu.edu

## Slide 2: Materials

## Slide 3: Bill of Materials
TPU95 flexible filament
540 mm of 1.5mm aluminum armature wire
Straps (examples listed below)
  4mm ID x 6mm OD Silicone rubber tube
  Non-latex resistance band
  Other strap materials are feasible, but only the two above have been tested

## Slide 4: Cost of Goods Sold (COGS)
Item | Supplier | Category | Price | Link
1.5mm x 550mm Armature wire | Animation Toolkit | Armature | $0.17 | https://tinyurl.com/yx7r4c38
Elastic cord 1/8” x 30” | Amazon | Strap | $0.04 | https://tinyurl.com/tf4ujzb
Polymaker PolyFlex 750 gram roll | Polymaker | Base | $1.80 | https://tinyurl.com/uvtl5es
Filter | ??? | Filter | ??? | ???

## Slide 5: 3D Printing

## Slide 6: Slicing Settings
Material: Polymaker PolyFlex
  Extruder: 250°C
  Bed: 60°C
Layers and perimeters
  Layer height: 0.3mm
  # Perimeters: 2
  Solid layers: 3 top and bottom
Infill
  Density: 25%
  Pattern: Rectilinear
Speed
  20mm/s for all speed settings
Print time: ≈3 hours
Material Used: 34 grams
Print Orientation

## Slide 7: Assembly